RUBBER CRUMB USED IN CONCRETE TO PROVIDE FREEZE-THAW PROTECTION (OPTIMUM PARTICLE SIZE)

Authors: Eli Dias & Alan Richardson – Northumbria University, Newcastle upon Tyne.

# 1. Introduction

This investigation is part of an ongoing research programme spanning five years at Northumbria University, which has looked into various aspects of rubber crumb usage in concrete with regard to freeze/thaw protection.  The research was carried to examine the optimum particle size of rubber crumb, when used within concrete, which will provide the maximum freeze-thaw protection. The investigation extends the range of earlier work carried out by Richardson, Coventry, and Ward, (2011) Richardson, Coventry, Dave, and Dave, J, (2011).

The rubber crumb used within the test was divided into five batches, where the concrete mix increased the rubber crumb size in instalments of 0.5mm. The range of rubber crumb used was between 0.5 to 2.5mm. The primary properties of the concrete investigated were; air content, freeze-thaw durability and compressive strength.

# 1. 1 Background

Vehicle tyres are made from a chemically improved rubber, and are designed to last for long periods of time (Waste watch, 2006). These specific properties pose difficult questions once the tyres have reached their end of life as they contain environmentally toxic substance, which in landfills break down very slowly and when they are incinerated, they produce dangerous pollutants (Siefle, 2006). The European Union identified this concern and took action by setting environmental legislation banning whole tyres from landfills from July 2003 and shredded tyres from July 2006 (Evans and Evans, 2006). Elbaba and Williams (2013) highlighted the severity of waste tyres as they suggest Europe and the USA combined produce approximately 8.3 million tons of waste tyres annually.

Since the early 1990’s numerous research has been carried out by many authors into the use of recycled rubber from vehicle tyres within concrete. These authors suggest the greatest characteristic benefits are: improved toughness, reduced density, greater sound absorption, increased ductility and reduced water absorbed (Fattuhi and Clark, 1996; Segre and Joekes, 2000; Khaloo, Dehestani and Rahmatabadi, 2008; Bravo and Brito, 2012; Mohammad et al, 2012). Furthermore, rubber incorporated into concrete have been proven to enhance the resistance to freeze-thaw deterioration (Paine and Dhir, 2010; Richardson et al, 2011).

It is believed rubber crumb has similar qualities to traditional air-entraining agents, which create minuscule pores (gel pores) that are so small temperatures can fall to -78oC without the formation of ice. These pores allow for the release of pressure and therefore protection from freeze-thaw attack (Neville and Brooks, 2010). Benazzouk et al (2006) highlighted the ability of rubber crumb particles to ‘artificially entrap air’. Khaloo, Dehestani and Rahmatabadi (2008) suggest this entrapping air is due to the non-polar rough surfaces of the rubber particles, which entrain air providing freeze-thaw protection.

Additionally, Benazzouk (2007) studied the hydraulic behaviour of rubber particles and discovered “rubber additives tend to restrict water propagation and reduce water absorption.”  Laźniewska-Piekarczyk (2013) explains this water repellent characteristic “will dramatically improve the durability of concrete exposed to moisture during cycles of freezing and thawing,” thus aiding the protection of concrete from freeze-thaw damage.

It is well recognised for every additional percent of entrained air added through air-entrainment agents, the compressive strength decreases by about five to six percent (Waddel and Dobrowolski, 1993; Cement admixtures associations, 2012). Similarly, since research started investigating the use of rubber within concrete it has been accepted there is a compressive strength loss. The overall consensus is the greater the quantity of rubber the larger the reduction in compressive strength. (Topçu, 1994; Fattuhi and Clark, 1996; Li, Li and Li, 1998; Khatib and Bayomy, 1999; Zheng, Huo and Yuan, 2008; Ganjian, Khorami and Maghsoudi, 2009; Atahan and Yücel, 2012; Bravo and Brito, 2012). However it must be noted, the majority of this research has used the rubber crumb as substitutes for fine or coarse aggregate.

The necessity to examine the rubber crumb particle was recognised by Fattuhi and Clark (1996) who recommend there’s a need to investigate the rubber in terms of ‘origin, size and shape’ and the effect each parameter has on concrete. Relatively little research has been carried out into these parameters, although Paine and Dhir (2010) suggested the freeze-thaw resistance increases as the rubber particle sizes decrease.  Zhu et al (2011) recognised that “the size of crumb rubber has an influence on the freeze-thaw resistance of concrete,” although this research introduced rubber as a sand replacement rather than additive.

This research was informed by Richardson, Coventry and Ward (2011) who investigated the optimum quantity of rubber crumb content for the most effective freeze-thaw protection was 0.6% by weight.

# 2. Methodology

To investigate if there is an optimum particle size of rubber crumb, several aspects of the concrete and materials were assessed. The rubber crumb was divided into five batches, increasing is instalments of 0.5mm, from > 0.5 to 2.5mm. The key elements for examination were: air content, freeze-thaw performance, compressive strength and rubber crumb distribution. Each element was subjected to tests as listed in Figure 1. These tests were based upon the British Standards Institution (BS) and American Society for Testing and Materials (ASTM).

Figure 1 – Test programme

A combination of ASTM C 666 and BS CEN/TR 15177:2006 were used to establish the principles of the freeze-thaw cycle. Time was a constraint with this research, so the initial decision was to follow the BS that recommended 56 cycles compared to the ASTM which states “300 cycles or until its relative dynamic modulus of elasticity reaches 60% of the initial modulus.” At the conclusion of 56 cycles the plan cubes had not failed, as the modulus of elasticity had not yet reached 60% of the initial modulus, therefore the test was extended for a further 14 cycles, to aid the deterioration of the cubes.

# 3. Results and Discussions

The density of concrete can be used to indicate the air content (Neville and Brooks, 2010). Figure 2 indicates the smaller the rubber crumb the greater the air entrainment, and consequently recommends the particle size > 0.5mm as offering the greatest freeze-thaw protection.

Figure 2 – Mean Density Comparison

The overall results for the air entrainment test are illustrated in Figure 3, which have produced a similar trend to the density test, which suggests the smaller the rubber crumb particle; the greater the air entrainment. The consistency between the density and air content results adds credence to the suggestion that > 0.5mm is the optimum particle size.

Figure 3 – Test programme

The pulse velocity for all batches over the specific test period can be seen in Figure 4. It is evident that the pulse velocity for all batches consistently increased over the first 42 cycles. Panzera et al (2011) suggests the causation of the pulse velocity increasing is due to a correlation between pulse velocity and increase in compressive strength. Due to the time constraints, the cubes started the freeze-thaw cycle after 3 days, which evidently continued to cure and increase in strength. However the most notable aspect of this test is the decrease in the plain cubes pulse velocity from cycle 42 to cycle 70, where for the same period the cubes with rubber crumb were relatively stable.

Figure 4 – Mean Pulse Velocity Comparison

During the freeze-thaw cycles all batches experienced a weight loss, although at different rates. The plain concrete cubes most meaningfully had the greatest loss, suggesting the most damage was caused, as illustrated in Figure 5.

Figure 5 – Mean Weight Loss Comparison

The full comparison of compressive strength, seen in Figure 6, is a great indication of the transformation the concrete cubes have undergone at different stages of this research. The increase of strength from the start of the freeze-thaw cycle at three days to the post freeze-thaw cycle strength reveals the concrete has continued to cure during at least part of the freeze-thaw cycles. The strength of the 28 day old cubes are stronger than the post freeze-thaw strength.

Figure 6 – Total Compressive strength Comparison

The >0.5mm rubber crumb additive achieved the best performing freeze/thaw performance as displayed in Figure 6.

# 4. Conclusion

There was no definitive correlation between the compressive strength and the rubber crumb particles size, although the rubberised concrete had an average strength loss of 5.24% after 28 days. Thus, this research indicates rubber crumb smaller than 0.5mm to be the optimum size to afford maximum freeze/thaw protection using a waste product within the concrete supply chain.

# References

American Society for Testing and Materials (2008) C666 – 97 Standard Test Method for Resistance of Concrete to Rapid Freezing and Thawing. Pennsylvania: American Society for Testing and Materials.

Atahan, A. O. and Yücel, A. Ö. (2012) ‘Crumb rubber in concrete: Static and dynamic evaluation’ Construction and Building Materials, 36, pp. 617-622.

Banazzouk, A., Douzane, O., Langlet, T., Mezreb, K., Roucoult, J. M. and Queneudec, M. (2007) ‘ Physico-mechanical properties and water absorption of cement composite containing shredded rubber wastes’ Cement & Concrete Composites, 29, pp. 732-740.

Benazzouk, A., Douzane, O., Mezreb, K. and Queneudec, M. (2006) ‘Physico-mechanical properties of aerated cement composites containing shredded rubber waste’ Cement & Concrete Composite, 28, pp. 650-657.

Bravo, M. and Brito, J. D. (2012) ‘Concrete made with used tyre aggregate: durability-related performance’ Journal of Cleaner Production, 25, pp. 42-50.

British Standards Institute (2006) PD CEN/TR 15177:2006 Testing the freeze-thaw resistance of concrete — Internal structural damage. London: British Standards Institute.

Elbaba, I. F. and Williams, P. T., (2013) ‘Hydrogen production from the pyrolysis-gasification of waste tyres with a nickel/dolomite catalyst’, Fuel, 103(April, 2013), pp. 528-536.

Evens, A. and Evens R, (2006) UK waste tyre management best practice: Handling of post-consumer tyres – collection & storage, Oxon: The waste & resources action programme.

Fattuhi, N. I. and Clark, L. A. (1996) ‘Cement-based materials containing shredded scrap truck tyre rubber’ Construction and Building Materials, 10(4), pp. 229-236.

Ganjian, E., Khorami, M. and Maghsoudi, A. A. (2009) ‘Scrap-tyre-rubber replacement for aggregate and filler in concrete’ Construction and Building Materials, 23, pp. 1828-1836.

Khallo, A. R., Dehestani, M. and Rahmatabadi, P. (2008) ‘Mechanical properties of concrete containing a high volume of tire-rubber particles’ Waste Management, 28, pp. 2472-2482.

Khatib, Z. K. and Bayomy, F. M. (1999) ‘Rubberized Portland cement concrete’, Journal of materials in civil engineering, 11, pp. 206-213.

Laźniewska-Piekarczyk, B.(2013) ‘The type of air-entraining and viscosity modifying admixture and porosity and frost durability of high performance self-compacting concrete’ Construction and Building Materials, 40, pp. 659-671.

Li, X., Li, F. and Li, J. S. L. (1998) ‘Properties of concrete incorporating rubber tyre particles’ Magazine of concrete research, 50, pp. 297-308.

Mohammed, B. S., Hossain, K. M. A., Swee, J. T. E., Wong. G and Abdullahi, M. (2012) ‘Properties of crumb rubber hollow concrete block’ Journal of Clean Production, 23, pp 57-67.

Neville, A. M. and Brooks, J. J. (2010) Concrete Technology. 2nd Ed. Essex: Pearson.

Paine, K. A. and Dhir, R. K. (2010) ‘Research on new applications for granulated rubber in concrete’ Construction Materials, 63(February), pp. 7-17, doi: 10.1680/coma.2010.163.1.73.

Richardson, A., Coventry, K. and Ward, G, (2011) ‘Freeze/thaw protection of concrete with optimum rubber crumb content’, Journal of Cleaner Production, 23(1, March 2012), pp. 96-103. doi: 10.1016/j.jclepro.2011.10.013

Richardson A.E., Coventry K., Dave U, Pineaar J, (2011), “Freeze/thaw protection of concrete using granulated rubber crumb”, The Journal of Green Building, Vol 6, Number 1, Winter, USA, pp 83 -92  doi/abs/10.3992/jgb.6.1.83

Segre, N and Joekes, I. (2000) ‘Use of tire rubber particles as addition to cement paste’ Cement and Concrete Research, 30, pp, 1421-1425.

Siegle, L (2006) Recycle the Essential Guide. London: Black Dog Publishing

Topcu, I. B. (1994) ‘The properties of rubberized concretes’ Cement and Concrete Research, 24(2), pp. 304-310.

Zheng, L., Huo, X. S. and Yuan, Y. (2008) ‘Strength, Modulus of Elasticity, and Brittleness Index of Rubberized Concrete’ Journal of Materials in Civil Engineering, 20, pp. 692-699.

Zhu, X., Miao, C., Liu, J. and Hong, J. (2011) ‘Influence of crumb rubber on frost resistance of concrete and effect mechanism’, Procedia Engineering, 23(2012), pp. 206-213.